## Slide 1
Photon echo quantum memories
S. A. Moiseev
Volga river
Kazan Quantum Center, Kazan National Research Technical University
named after A.N. Tupolev, 10 K. Marx Street, Kazan 420111, Russia, Russia
2 0 1 4
KQC

## Slide 2
Kazan Quantum Center KNRTU-KAI
Dr. N.M.Arslanov, К. I. Gerasimov, Dr. V.Gleim,
N. S. Perminov – senior scientists, M. S. Smirnov – engineer,
М. М. Мinnegaliev – PhD student, R.V.Urmancheev –PhD student.
Kazan Federal University, Russia,
Prof. B. Z. Malkin, Prof. O.N. Sherstyukov, Dr. S. L. Korableva, Dr. E. I. Baibekov,
PhD students: R.R. Latypov, K.V. Petrovnin, and Е. S. Моiseev,
Kazan Physical-Technical Institute of RAS, Russia,
Dr. F.F.Gubaidullin, N.S.Perminov – senior scientists
ITMO University, Department of Photonics and Optical Information Technology, Saint Petersburg, Russia
Prof. S.A.Kozlov, Dr. V.Gleim, (quantum communication group)
Institute for Perspective Studies of Science Academy of Tatarstan Republic, Russia,
Prof. S. N. Аndrianov,
Laboratoire Aimé Cotton, CNRS, Univ. Paris-Sud, Orsay, France
Prof. T. Chanelière, Dr. A. Louchet-Chauvet (quantum memory group)

## Slide 3
Quantum memory
For optical quantum computing (P.Kok, et al, RMP, 79 135 (2007)),
Quantum repeaters (H.-J., Briegel, et.al, PRL, 81, 5932 (1998))
Quantum network (H.J. Kimble, Nature 453, 1023 (2008)).
For microwave quantum computing (B. Julsgaard, Y. Kubo, et al., Phys. Rev. A 92, 020301 (2015); Review: arXiv:1510.06565v1).
Quantum memory for universal quantum computer
C.A. P´erez-Delgado and P. Kok, Phys. Rev. A 83, 012303 (2011)

## Slide 4
Current status:
1. Nanosecond time scale,
2. Efficiency ~ 90 % recovery fidelity ~ 97%;
3. 1000-light temporal modes are possible, there are a number of experiments with 10-100 photonic qubits;
4. The first experiments on the implementation of QM in optical waveguides, resonators ... (so far with low efficiency);
5. Rare earth ions in inorganic crystals, P in Si,
NV-centers in diamond;
6. Storage time up to a few hours is possible , usually ~ 1 ms; There are experiments with 1 sec. cesium (low QE~3%); 1 sec. Pr:YSO (Helium temp, low eff.)
7. Helium temp.: solid state media,
room temp.: NV-centers, atomic gases: Rb; cesium (low QE~3%)
8. Simple linear manipulations are demonstrated (GEM protocol); there are a number of proposed schemes.
9. In progress;
10. In progress, there are first promising experiments.
(QE~16.5%)
1. High operation rate;
2. High efficiency and fidelity (>99.99%);
3. Multimode capacity;
4. Integration in a quantum scheme, the implementation in the circuits on the chip and nanometer level;
5. Solid state quantum information carrier;
6. Long lived storage (> 1 msec needed for qu.repeater);
7. Temperature of QM medium;
8. Using quantum memory for simple quantum manipulations;
9. Implementation of quantum repeaters based on optical quantum memory;
10. QM for superconducting quantum computing.
…
Квантовая память: основные требования

## Slide 5
[1]. Lvovsky Alexander I., Sanders Barry C., Tittel Wolfgang. Optical quantum memory //Nat. Pho­tonics.- 2009. - dec. - Vol. 3, no. 12. - Pp. 706-714.
[2]. Hammerer Klemens, Sorensen Anders S., Polzik Eugene S. Quantum interface between light and atomic ensembles //Rev. Mod. Phys.- 2010. - Apr. - Vol. 82. - Pp. 1041-1093.
[3]. Quantum memories / Simon, C., Afzelius, M., Appel, J. et al. //Eur. Phys. J. D.- 2010. - Vol. 58, no. 1. - Pp. 1-22.
[4]. Photon-echo quantum memory in solid state systems / W. Tittel, M. Afzelius, T. Chaneliere et al. //Laser & Photonics Reviews.- 2010. - Vol. 4, no. 2. - Pp. 244-267..
[5]. Prospective applications of optical quantum memories / F. Bussieres, N. Sangouard, M.Afzelius et al. // J. Mod. Opt.- 2013. - oct. - Vol. 60, no. 18. - Pp. 1519-1537.
[6]. K. Heshami, D.G. England, P.C. Humphreys et al. Quantum memories: emerging applications and recent advances. // J. Mod. Opt.- 2015. - preprint.http://arxiv.org/abs/1511.04018.
[7] Lijun Ma, Oliver Slattery and Xiao Tang, Optical quantum memory based on electromagnetically induced transparency J. Opt. 19 (2017) 043001 (24pp)
[8] T Chanelière, G Hétet, N Sangouard Quantum optical memory protocols in atomic ensembles - arXiv preprint arXiv:1801.10023, 2018 - arxiv.org
Reviews on quantum memory
Special issues on QM
[1]. Quantum memory J. Phys. B: At. Mol. Opt. Phys.- 2012. - Vol. 45. - Pp. 120201-124021.
[2]. Focus on Quantum memory New J. Phys.- 2015. - Vol. 17. - P. 050201.
[3]. Special Issue CFP: Quantum Memory, Journal of Modern Optics. – 2016.

## Slide 6
Chen Y-H et al 2013 Phys. Rev. Lett. 110 083601 (QE=78%)
EIT based Quantum Memory
M. Fleischhauer and M. D. Lukin, PRL. 84, 5094, (2000).
Photon Echo Quantum Memories
S.A.Moiseev and S.Kroll, PRL. 87, 173601, (2001)- Basic scheme (CRIB).
W. Tittel, M. Afzelius, T. Chaneliere , R.L.Cone, S.Kroll, S.A.Moiseev, and M.Sellars.
Laser & Photonics Reviews.- 2010. 4, 244-267..
M.Hosseini et al Nature Commun. 2, 174 (2011) CRIB/GEM (QE - 87%)
A.E.Kozhekin, K. Molmer, and E.S.Polzik, Phys. Rev. A 62, 033809 (2000).
Reim K F, et al., A Phys. Rev. Lett. 107 053603 (2011) (QE=30%)
Off-resonant Raman scheme
A.Gorshkov, A Andre, M Fleishhhauer, A.S.Soensen and M.D.Lukin PRL 98, 123601 (2007).
A.Kalachev Phys.Rev.A. 76, 043812 (2007).
T.Golubeva, Yu. Golubev, O.Mishina, A.Bramati, J.Laurat, and E.Giacobino,
Phys. Rev. A 83, 053810 (2011).
High-speed atomic memory
Optical quantum memory based on atomic ensembles
time
input
control
control
output

## Slide 7
Chen Y-H et al 2013 Phys. Rev. Lett. 110 083601 (QE=78%)
EIT based Quantum Memory
M. Fleischhauer and M. D. Lukin, PRL. 84, 5094, (2000).
Photon Echo Quantum Memories
S.A.Moiseev and S.Kroll, PRL. 87, 173601, (2001)- Basic scheme (CRIB).
W. Tittel, M. Afzelius, T. Chaneliere , R.L.Cone, S.Kroll, S.A.Moiseev, and M.Sellars.
Laser & Photonics Reviews.- 2010. 4, 244-267..
M.Hosseini et al Nature Commun. 2, 174 (2011) CRIB/GEM (QE - 87%)
A.E.Kozhekin, K. Molmer, and E.S.Polzik, Phys. Rev. A 62, 033809 (2000).
Reim K F, et al., A Phys. Rev. Lett. 107 053603 (2011) (QE=30%)
Off-resonant Raman scheme
A.Gorshkov, A Andre, M Fleishhhauer, A.S.Soensen and M.D.Lukin PRL 98, 123601 (2007).
A.Kalachev Phys.Rev.A. 76, 043812 (2007).
T.Golubeva, Yu. Golubev, O.Mishina, A.Bramati, J.Laurat, and E.Giacobino,
Phys. Rev. A 83, 053810 (2011).
High-speed atomic memory
Optical quantum memory based on atomic ensembles
time
input
control
control
output

## Slide 8
CRIB
Complete absorption within IB line
Inversion of IB line
Backward echo field emission
AFC
Complete absorption within IB line
Backward echo field emission
IB line consists of periodic structure of narrow lines
Perfect time reversibility
PEQM on natural IB (ROSE,…)
Complete absorption within IB line
Backward echo field emission
+ Rephasing by sequence of intensive laser pulses
GEM
Complete absorption within IB line
Inversion of IB line
+ IB is determined by controllable gradient of Stark (Zeeman) shifts
Off-resonant Raman echo M
promising properties:
1. Provides generalized time reversibility
2. It can be used for CRIB/GEM, AFC, ROSE protocols
3. Provides a direct storage on long-lived levels
(2008)
(2001,)
(2006)
(2008,2012)
(2011)
1) Microwave multiresonator
2) On-chip multi-ring optical scheme
(2017,2018)
Impedance matching schemes
promising properties:
Small size samples
2. Perfect integration
(2010)
Схемы квантовой памяти на фотонном эхе

## Slide 9
Some recent experiments on photon echo quantum memories
2010-2017:
Most efficient quantum memory for light in a crystal (69 %).
M.Hedges, et al, Nature 465, 1052–1056 (2010).
Quantum storage of photonic entanglement in a crystal.
C. Clausen, et al. Nature 469, 508–511 (2011).
A. Tiranov, et al, . arXiv:1606.07774v2
Integration of rare-earth ions in the optical waveguides for implementation of photon echo protocols
E. Saglamyurek, et al, Nature (London) 469, 512-515 (2011).
Towards elaboration of optical quantum repeaters based on the photon echo approaches in the crystals doped by rare-earth ions:
N. Sinclair, et al, Phys. Rev. Lett. 113, 053603 (2014).
E. Saglamyurek, et al, Nat. Commun. 7, 13454 (2015).
Optical waveguides created in inorganic crystal with rare-earth ions:
G. Corrielli, et al., Phys. Rev. Applied 5, 054013 (2016).
Towards non-destructive detection of photonic qubits based on AFC photon echo in Tm:LiNbO3 waveguide
Sinclair, N. et al.. Nat. Commun. 7, 13454 (2016).
Tian Zhong, et.al.,Interfacing broadband photonic qubits to on-chip cavity-protected rare-earth ensembles. Nat. comm. Sep. 2016. doi:10.1038/ncomms14107 (2016)
Tian Zhong, et.al., Nanophotonic rare-earth quantum memory with optically controlled retrieval. Science, August 2017.doi: 10.1126/science.aan5959(2017). (2017)

## Slide 10
Towards microwave spin echo quantum memory
Spin ensembles in microwave QED cavity
Y. Kubo, et al, Phys. Rev. Lett. 105, 140502 (2010).
D. I. Schuster, et al, Phys. Rev. Lett. 105, 140501 (2010).
B. Julsgaard, C. Grezes, P. Bertet, and K. Mølmer, Phys. Rev. Lett. 110, 250503 (2013).
M. Afzelius, N. Sangouard, G. Johansson, M. U. Staudt, and C. M. Wilson, New J. Phys. 15, 065008 (2013).
S. Probst, et. Al, Phys. Rev. Lett. 110(15), 157001 (2013).
K.I. Gerasimov, S.A. Moiseev, V.I. Morosov, R.B. Zaripov, Phys. Rev. A 90(4), 042306 (2014).
C. Grezes, et al, Phys. Rev. A 92(2), 020301 (2015).
Arcangeli, A., Ferrier, A. & Goldner, Phys. Rev. A 93, 062303 (2016).
Krimer, D. O., Zens, M., Putz, S. & Rotter, S. Laser & Photonics Rev. 10, 1023–1030 (2016).
Gerasimov, K.I., Moiseev, S.A. & Zaripov, R.B. Appl Magn Reson Volume 48, No. 795(2017).
Quantum memory with millisecond coherence in circuit QED
Matthew Reagor, et al, Phys.Rev.A. B 94, 014506 (2016)

## Slide 11
Basic properties of quantum memory media
external electric (E) and (or) magnetic (B) fields
To
Resonant atoms
single photons
and control laser fields
Quantum efficiency:
where
Fidelity:
in
in
out
out
Atomic levels
|1>
|2>
|3>

## Slide 12
Arsenal of coherent optical effects:
Coherent effects in multi-two level atomic systems:
Free induction decay, spin/photon echoes,
Dicke superradiance, Slow light, off-resonant Raman interaction…
Esignal 21
|2 j >
|1 j>
Atomic Hamiltonian:
G(-o)
(-j)

Inhomogeneous and homogeneous broadening of resonant line
Light spectrum

## Slide 13
Photon Echo Quantum Memory
(CRIB scheme AFC, Roze, Raman protocols, other variants)
S.A.Moiseev and S.Kroll, Phys.Rev.Lett.(2001).
1
 2
3
Esignal
E1
E2
Eecho
j(t’)
-j(t)

(-t)=0
t > to:
  - 
Time
to
Spatial Reversible (Backward) Scheme of Photon Echo:
Notes: 13

## Slide 14
E1
Medium
Spatial reversible (backward) free space scheme of photon echo QM:
Resonant absorption
1
 2
3
E1
Esignal
G(-o)

Esignal

## Slide 15
E1
Medium
Resonant absorption
1
 2
3
E1
G(-o)

Esignal
Spatial reversible (backward) free space scheme of photon echo QM:

## Slide 16
Medium
Resonant absorption
1
 2
3
E1
E2
Eecho
G(-o)

Esignal
E1
Spatial reversible (backward) free space scheme of photon echo QM:

## Slide 17
Medium
Resonant absorption
1
 2
3
E1
E2
Eecho
G(-o)

Esignal
-:
Spatial reversible (backward) free space scheme of photon echo QM:

## Slide 18
Medium
Resonant absorption
1
 2
3
E1
E2
Eecho
G(-o)

Esignal
-:
E2
Spatial reversible (backward) free space scheme of photon echo QM:

## Slide 19
Medium
Resonant absorption
1
 2
3
E1
E2
Eecho
G(-o)

Esignal
-:
E2
Spatial reversible (backward) free space scheme of photon echo QM:

## Slide 20
Medium
Resonant absorption
1
 2
3
E1
E2
G(-o)

Esignal
-:
E2
Eecho
Eecho
Time reversal dynamics  time reversal shape of the output light pulse
Spatial reversible (backward) free space scheme of photon echo QM:

## Slide 21
Absorption
stage
Echo
emission
Photon Echo Quantum Memory
S.A.Moiseev, M.I. Noskov. Laser Physics Letters (2004), 1, № 6, 303-310
Maxwell-Bloch equations

## Slide 22
Absorption
stage
Echo
emission
Photon Echo Quantum Memory
S.A.Moiseev, M.I. Noskov. Laser Physics Letters (2004), 1, № 6, 303-310
 - , Eecho - Eo t - t
-B.Kraus, et.al., PRA. 73, 020302(R) (2006).
Maxwell-Bloch equations

## Slide 23
Maxwell-Bloch equations
Absorption stage
Excited atomic coherence:
Absorption effect
Dispersion
Dephasing
S.A.Moiseev, M.I. Noskov. Laser Physics Letters (2004), 1, № 6, 303-310
S. A. Moiseev, and J.-L. Le Gouët, J. Physics B: At. Mol. & Opt. Phys 45, 124003, (2012)

## Slide 24
Some basic properties of CRIB
Echo signal irradiation
1
 2
3
E1
E2
Eecho
Large optical depth: L>>1
Misphasematching

## Slide 25
Basic properties of free space photon echo QM
Echo signal irradiation
1
 2
3
E1
E2
Eecho
Medium
Resonant absorption
ks
kecho
k1
k2
k2
-k1
ks
kecho
kecho = ks – k1+ k2
Large optical depth: L>>1
Misphasematching

## Slide 26
The retrieved quantum state
Arbitrary initial quantum state of light:
12
1
)
'
(
)
,
n(
c
k
x
n
t
t
c
k
t
n
m
m
-
-
=
å
=
Spectrum:
Initial field Photon echo field


22
S.A. Moiseev. J. of Phys. B: Atom., Mol. & Opt. Phys. 40, 3877-3891 (2007).

## Slide 27
Maxwell-Bloch equations
Gaussian inhomogeneous broadening
Natural IB
Gradient Memory
Atomic frequency Comb
G()
in
Linewidth
A.L.Alexander, et al,
PRL(2006).
H. De Riedmatten, et al.,
Nature (2008)
G()
S. A. Moiseev, PRA (2011).
D. L. McAuslan, et.al, PRA (2011).
V. Damon et al., NJP (2011).

## Slide 28
Maxwell-Bloch equations
Gaussian inhomogeneous broadening
Natural IB
Gradient Memory
Atomic frequency Comb
G()
in
Linewidth
A.L.Alexander, et al,
PRL(2006); S.A. Moiseev, and N.M. Arslanov. PRA. 78, 023803 (2008).
.
H. De Riedmatten, et al.,
Nature (2008)
G()
S. A. Moiseev, PRA (2011).
D. L. McAuslan, et.al, PRA (2011).
V. Damon et al., NJP (2011).
Useful for broadband storage

## Slide 29
Quantum storage of 64 light pulses: I.Usmani, M.Afzelius, H.de Riedmatten, and N.Gisin, Nature Comm.1,1 (2010) (Nd 3+ :YVO 4 crystal).
Quantum storage of 1064 temporal light modes:
M. Bonarota, J.-L. Le Gouet, and T. Chaneliere, New J of Physics 13 (2011) 13013
Photon Echo QM for multi-mode light fields. Experimental demonstration of quantum storage
Experiments with highest quantum efficiency
M. Hosseini, B. M. Sparkes, P. K. Lam, and B. C. Buchler, Nature Commun.1,1, (2011) (gas, room temperature, quantum efficiency = 87 %, storage time ~ few s).
Y.-W. Cho , et al , Optica, ol. 3, No. 1, 100, (2016) (cold gas, quantum efficiency = 87 % storage time ~ 1 ms).

## Slide 30
G(/in)
o
in



резкость F=/
S. A. Moiseev, and J.-L. Le Gouët, J. Physics B: At. Mol. & Opt. Phys 45, 124003, (2012)
Н.М. Арсланов, С.А.Моисеев, Квантовая Электроника, Том 47, № 9, с. 783-789 (2017).
К широкополосной эффективной квантовой памяти
на AFC протоколе
Проект улучшения AFC протокола

## Slide 31
G(/in)
qm
o
in

К широкополосной эффективной квантовой памяти
на AFC протоколе
Проект улучшения AFC протокола
Н.М. Арсланов, С.А.Моисеев,
Кв. Электроника 47, 783 (2017).

## Slide 32
.
Карты расчета максимальной ширины квантовой памяти qm
и значений АЧГ (AFC) структуры 0 для двух значений эффективности 10%, 90% в зависимости от оптической плотности L и резкости f cтруктуры
Карта максимальной ширины qm при оптимальной 0 в единицах in. Стрелки указывают на изолинии максимальных значений Δopt0 для различной эффективности = 10% (а) и 90% (б).
Н.М. Арсланов, С.А.Моисеев, Оптика и спектроскопия (2019 в печати).

## Slide 33
Photon echo QM in optimal QED cavity
resonant atoms
semitransparent mirror
mirror
photons
Resonant line of single monochromatic atomic group
Inhomogeneously broadened line

in
cavity mode

N - number of atoms
g – coupling constant
of atom-photon interaction
|1>
|2>

Cavity schemes
S.A. Moiseev, S.N. Andrianov, and F.F. Gubaidullin Phys. Rev. A 82, 022311 (2010) (CRIB)
M.Afzelius, C.Simon Phys. Rev. A 82, 022310 (2010) (AFC)

## Slide 34
S.A. Moiseev. Phys.Rev.A 88, 012304 (2013).
Off-resonant Raman echo QM in single mode cavity

## Slide 35
S.A. Moiseev. Phys.Rev.A 88, 012304 (2013).
Off-resonant Raman echo QM in single mode cavity
A.E.Kozhekin, K. Molmer, and E.S.Polzik, Phys. Rev. A 62, 033809 (2000).
S.A.Moiseev and S.Kroll, PRL. 87, 173601, (2001)
+ cavity

## Slide 36
Hamiltonian (quantum optics)
Inhomogeneous and homogenous broadenings
Atom-cavity mode interaction
k=1- external (waveguide) modes; 2- bath modes
Perturbation and interaction parts:
Spectral detunings of the field modes
Interaction of cavity mode with other field modes
Basic Hamiltonian of atoms (electron spins) and photon fields
Notes: 36

## Slide 37
Quantum efficiency
where:
- is a total spectral width, including inhomogeneous broadening
Spectral efficiency Z(,…,):
Storage:
Notes: 37

## Slide 38
It has been found that two impedance matching conditions should be satisfied for
Broadband efficient quantum memory:
Basic impedance matching:
Spectral matching condition:

in
Z (,…)
Photon echo QM in optimal QED cavity
Spectral efficiency of quantum memory
resonant atoms
mirror
Echo photons
cavity mode


(CRIB)
(AFC)

## Slide 39
39
Fabry-Perot cavity (on crystal surfaces) 0.05 % Pr3+ : Y2SiO5) :
Sabooni M., Li Q., Kroll S and Rippe L. Phys. Rev. Lett. 110 133604 (2013)
Sabooni M., Kometa S.T., Thuresson A., Kroll S. and Rippe L. New Journal of Physics 15, 035025 (2013).
Finesse F=/=4.5
Rephasing (reemission) time:
(QE=58%)
Quantum efficiency =58% (Record for AFC-protocol)
First experiments
External optical cavity
P. Jobez, I. Usmani, N. Timoney, C. Laplane, N. Gisin, M. Afzelius. New Journal of Physics 16, 083005 (2014) (QE=53%)
R A Akhmedzhanov, L A Gushchin, A A Kalachev, N A Nizov, V A Nizov, D A Sobgayda and I V Zelensky, Laser Phys. Lett. 13, 115203 (2016). (QE=3% for 10 nsec pulse)

## Slide 40
Recent experiments on microwave spin echo quantum memory on NV-centers
C. Grezes, B. Julsgaard, Y. Kubo, et al., Multimode Storage and Retrieval of Microwave Fields in a Spin Ensemble Phys.Rev.X, 4, 021049 (2014).
Grezes, B. Julsgaard, Y. Kubo, et al., Storage and retrieval of microwave fields at the single-photon level in a spin ensemble Phys. Rev. A 92, 020301 (2015); Review: arXiv:1510.06565v1 . Quantum efficiency– 0.3 %
Towards microwave quantum memory for superconducting quantum computer

## Slide 41
Impedance matching quantum memory
S.A. Moiseev, S.N. Andrianov, and F.F. Gubaidullin Phys. Rev. A 82, 022311 (2010)
Первые подтверждающие эксперименты
Sabooni M., Li Q., Kroll S and Rippe L. Phys. Rev. Lett. 110 133604 (2013)
P. Jobez, I. Usmani, N. Timoney, C. Laplane, N. Gisin, M. Afzelius. New Journal of Physics 16, 083005 (2014)
R A Akhmedzhanov, L A Gushchin, A A Kalachev, N A Nizov, V A Nizov, D A Sobgayda and I V Zelensky, Laser Phys. Lett. 13, 115203 (2016).
S. A. Moiseev, and S.N. Andrianov. J. Phys. B: At., Mol. & Opt Phys. 45, 124017 (9pp) (2012)
E. S. Moiseev & S. A. Moiseev Journal of Modern Optics, 63, No. 20, 2081–2092. (2016):
S.A.Moiseev and S.N. Andrianov Optics and Spectroscopy, Vol. 121, No. 6, pp. 886–896 (2016).
Integrated QM and multi-qubit quantum RAM
New quantum memory schemes on photon/spin echo
for integration in quantum circuits

## Slide 42
09.03.2015
Impedance matching
Spectral impedance matching :
Квантовая РАМ на фотонном эхе в резонаторах
Optical scheme (and microwave scheme)
Control
atom
Atomic ensemble
ph = 31 = o  j
E. S. Moiseev, and S. A. Moiseev. Time-bin quantum RAM. Journal of Modern Optics, 63, No. 20, 2081–2092 (2016).
Проект

## Slide 43: Optical scheme
and determine temporal duration of laser pulse (-1) and its spectral width - 2.
These parameters have been controlled experimentally.
кристалл Y3Al5O12: Tm3+
crystal
Crystal
Digital
oscilloscope
Spectral width
1GHz
Detector
Cryostat
Input
pulse
echo
Controlling laser pulses
Signal field
Generator of pulses
with arbitrary shape
linewidth 5KHz
Ti-Sp Laser
Bus of automatic control
beamsplitter
Experimental setup for observation of Scilenced photon echo in orthogonal geometry of laser field control
K. I. Gerasimov , M. M. Minnegaliev , S. A. Moiseev , R. V. Urmancheev, T. Chanelière, and A. Louchet-Chauve
Quantum Memory in Orthogonal Geometry of Scilenced Echo Retrieval Optics and Spectroscopy, 2017, Vol. 123, No. 2, pp. 209–215.
Our first experiment towards the photon echo QM in optical cavity

## Slide 44
Ie = I0  exp (-2( t / Tm )x)
Tm= 55 мкс, x = 1.8
Максимальная эффективность
39.4 %
Normalized intensity
Intensity of input signal
Intensity of input signal reflected from resonator and signal of photon echo
Echo pulse
Efficiency – 21 %
Maximum efficiency – 39.4 %
ROSE- photon echo protocol
On crystal Y3Al5O12: Tm3+ in optical resonator
M.M. Minnegaliev, K.I. Gerasimov, R.V.Urmancheev, and S.A. Moiseev. Quantum memory in scheme of silenced echo retrieval in optical resonator. Quantum Electronics (2018, in press).

## Slide 45
S.A. Moiseev. Phys.Rev.A 88, 012304 (2013).
Off-resonant Raman echo QM in single mode cavity
(towards using crystal with rare-earth ions)
Storage on
Long-lived levels
проект в резонаторе:

## Slide 46
S.A. Moiseev. Phys.Rev.A 88, 012304 (2013).
A.E.Kozhekin, K. Molmer, and E.S.Polzik, Phys. Rev. A 62, 033809 (2000).
S.A.Moiseev and S.Kroll, PRL. 87, 173601, (2001),
S.A. Moiseev, S.N. Andrianov, and F.F. Gubaidullin Phys. Rev. A 82, 022311 (2010)
S. A. Moiseev, and W. Tittel. New J Phys. 13, 063035 (2011).
Off-resonant Raman echo QM in single mode cavity
(towards using crystal with rare-earth ions)
Storage on
Long-lived levels
проект в резонаторе:

## Slide 47
S.A. Moiseev. Phys.Rev.A 88, 012304 (2013).
Modified impedance matching:
Spectral impedance matching :
Possiblity of realization in crystals with rare-earth ions :

in
Z (,…)
in(13) < 24 Mhz for Er ions!
o 10 in(13) =24 10 7 Hz.
Квантовая память на нерезонансном рамановском эхе в резонаторе
Spectral efficiency of quantum memory
проект в резонаторе:

## Slide 48
Temporal scheme of interaction
t
2
3
6
4
5
1
T0
t0
Signal
Echo
k
k+2T0
2 2c
3 3c
Lz
to
3 3c
|3>
 0
|2
|1
t
2
3
2 2c
 0,2

## Slide 49
Spectral range of effective storage
Quantum efficiency
Fidelity

## Slide 50
Пространственное кодирование фотонных кубитов
1-st
2-nd
3-rd
1-st
2-nd
3-rd
Стадия сохранения фотонных кубитов :
Схема реализации селективной многомодовой КП на нерезонансном рамановском эхе в резонаторе
Проект

## Slide 51
Broadband Raman echo quantum memory in white QED cavity
С.А.Моисеев, Е.С.Моисеев. Труды 5-й Международной конференции «Современные нанотехнологии и нанофотоника для науки и производства» 12-15 ноября, 2016, Владимир, Россия сс. 207-2011
E. S. Moiseev, S. A. Moiseev, K.I.Gerasimov, A.Tashchilina, and M.Sabooni. Broadband Raman echo quantum memory in white QED cavity (submitted in press)
Two control fields are applied simultaneously
Signal field
S
C
|1
|4
|2
|5
|3
|6
C
S
C
C
S
Проект

## Slide 52
Численные расчеты:
(Широкополосная КП на нерезонансном рамановском эхе в «белом» резонаторе)

## Slide 53
Численные расчеты:
(Широкополосная КП на нерезонансном рамановском эхе в «белом» резонаторе)
Мода резонатора
Сигнальное поле

## Slide 54
Численные расчеты:
(Широкополосная КП на нерезонансном рамановском эхе в «белом» резонаторе)

## Slide 55
Численные расчеты:
(Широкополосная КП на нерезонансном рамановском эхе в «белом» резонаторе)

## Slide 56
Multi-resonator quantum memory
E. S. Moiseev, and S. A. Moiseev, Laser Phys. Lett. 14, 015202 (2017)
S.A. Moiseev, F.F. Gubaidullin, R.S. Kirillov, R.R. Latypov, N.S. Perminov, K.V. Petrovnin, O.N. Sherstyukov.
Phys.Rev.A. 95, 012338 (2017).
S.A.Moiseev, K.I. Gerasimov, R.R. Latypov, N.S. Perminov, K.V. Petrovnin, and O.N. Sherstyukov. Scientific Reports V.8, 3982 (2018)
Petrovnin K, Perminov N, Sherstyukov O and Moiseev S Quantum Electronics 2018 (in press)
New quantum memory schemes on photon/spin echo
for integration in quantum circuits

## Slide 57
b1
b2
bn-1
bn




Spectrum of
input signal
S. Moiseev, E. Moiseev Laser Phys. Lett. 14 (2017) 015202
CRC-протокол
Developing broadband multi-resonator quantum memory

## Slide 58
Demonstration of effective storage of three-pulse input field
Number of cavities: N = 61
Finesse: F=/(2) = 50
Spectral width: =10

## Slide 59
=0.5
=0.25
=0.1
techo 60 ts = -1
Optimal coupling of ring cavity with optical waveguide (impedance matching):

## Slide 60
=0.5
(impedance matching condition): =0.5
1 N




Optimal coupling of ring cavity with optical waveguide (impedance matching):
Time window
for manipulation with field trapped in a system of high Q miniresonators
Cascade quantum memory

## Slide 61
b1
b2
bn-1
bn




S. Moiseev, E. Moiseev Laser Phys. Lett. 14 (2017) 015202
Multi- ring resonator scheme of QM
Towards optical and microwave quantum memories :
=0.5
=0.25
=0.1
techo 60 ts = -1

## Slide 62
b1
b2
bn-1
bn




Multi- ring resonator scheme of QM
Towards optical and microwave quantum memories :
This version of memory we implemented on a system of microwave ring resonators with an efficiency of 3 %. Optical quantum memory on a system of high-quality resonators will be able to operate at room temperature with a storage time of up to 100 µs.
=0.5
=0.25
=0.1
techo 60 ts = -1
Microwave scheme
First experiment:
K.V. Petrovnin, N.S. Petrovnin, O.N.Sherstukov, and S.A.Moiseev, Microwave quantum memory on controlled frequency combs, Quantum Electronics (2018, in press).
S. Moiseev, E. Moiseev Laser Phys. Lett. 14 (2017) 015202

## Slide 63
Spin ensembles in microwave QED cavity:
With natural AFC spin system:
K.I. Gerasimov, S.A. Moiseev, V.I. Morosov, R.B. Zaripov, Phys. Rev. A 90(4), 042306 (2014).
Gerasimov, K.I., Moiseev, S.A. & Zaripov, R.B. Appl. Magn. Reson. 48, 795 (2017).
Multiresonator quantum memory,
Moiseev, S. A., Gubaidullin, F. F., Kirillov, R. S., Latypov, R. R., Perminov, N. S., Petrovnin, K. V., and Sherstyukov, O. N., Phys. Rev. A 95, 012338 (2017). All-optical photon echo on a chip,
Moiseev, E. S. and Moiseev, S. A., Laser Physics Letters 14(1), 015202 (2017).
Spectral-topological superefficient quantum memory,
Perminov, N. S. and Moiseev, S. A., (2017) (sent to PRL).
Broadband multiresonator quantum memory-interface,
Moiseev, S. A., Gerasimov, K. I., Latypov, R. R., Perminov, N. S., Petrovnin, K. V., and Sherstyukov, O. N., (2017) (sent to Sci. Rep.).
Superefficient long-lived multiresonator quantum memory,
N.S. Perminov, D.Yu. Tarankova, S.A. Moiseev, (2017) (Proc. of SPIE); arxiv:1711.07014, (2017).
N.S. Perminov, D. Yu. Tarankova, S. A. Moiseev. Superefficient cascade multiresonator quantum memory Las.Phys.Lett. (2019) arXiv:1809.08759
On the way to microwave multi-resonator quantum memory

## Slide 64
2 0 1 4
KQC
Periodic spatial and frequency location
zn = z0 + n  , n = 0 + n 
S.A. Moiseev, F.F. Gubaidullin, R.S. Kirillov, R.R. Latypov, N.S. Perminov, K.V. Petrovnin and O.N. Sherstyukov, Multiresonator Quantum Memory, Phys.Rev.A. 95, 012338 (2017)
Bragg type impedance matching condition:
1 N



Light field
Light field
Microwave multiresonator protocol
= /2

## Slide 65
2 0 1 4
KQC
Compact resonators (Q = 2103 )
Common microwave waveguide (=3 cm)
L=10 cm
Tuning tools
Towards mutiresonant microwave quantum memory
S. A. Moiseev, F. F. Gubaidullin, R. S. Kirillov, R. R. Latypov, N. S. Perminov, K. V. Petrovnin, and O. N. Sherstyukov, Phys. Rev. A 95, 012338 (2017)
Numerical Simulations of electromagnetic field
Magnetic field Electric field
Common resonator + 6 coupled miniresonators
Single miniresonator

## Slide 66
2 0 1 4
KQC
9.73 Ghz
5 Mhz
1 Mhz
T=300 K
Experimental spectra of the multiresonator system

## Slide 67
2 0 1 4
KQC
Experimental normalized echo intensity
nanoseconds
Quantum Efficiency ~ 16.3 %
S.A. Moiseev, K.I. Gerasimov, R.S. Kirillov, R.R. Latypov, N.S. Perminov, K.V. Petrovnin, O.N. Sherstyukov. “Broadband multiresonator quantum memory-interface” Scientific Reports V.8, # 3982 (2018).

## Slide 68
2 0 1 4
KQC
Recent experimental data on AFC microwave protocol
S.A. Moiseev, K.I. Gerasimov, R.S. Kirillov, R.R. Latypov, N.S. Perminov, K.V. Petrovnin, O.N. Sherstyukov. “Broadband multiresonator quantum memory-interface” Scientific Reports V.8, # 3982 (2018).
Experimental normalized echo intensity
nanoseconds
Quantum Efficiency ~ 16.3 %
Time window
for manipulation with field trapped in a system of high Q miniresonators

## Slide 69
2 0 1 4
KQC
Experimental normalized echo intensity
nanoseconds
Quantum Efficiency ~ 16.3 %
Recent experimental data on AFC microwave protocol

## Slide 70
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
1 N


AFC (infinite number of combs)
in resonator
M. Afzelius and C. Simon, Phys. Rev. A, 82, 022310 (2010).
Towards superefficient quantum memory
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv:1706.00592


## Slide 71
Towards superefficient quantum memory
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
1 4


|f()|2
1 4
Small number of combs (N=4)
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv:1706.00592


## Slide 72
Towards superefficient quantum memory
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv:1706.00592
1 4


|f()|2
1 4
Small number of combs (N=4)
Squeezing of
spectral distances
due to strong coupling
with cavity mode


## Slide 73
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv: 1706.00592
 ±1 = = ±0.5,  ±2 = ±1.5,
g±1 = 0.318, g±2 = 0.318
Initially periodic comb structure
Towards superefficient quantum memory

## Slide 74
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv: 1706.00592
 ±1 = ±0.5,  ±2 = ±1.92,
g±1 = 0.318, g±2 = 1.09
 ±1 = = ±0.5,  ±2 = ±1.5,
g±1 = 0.318, g±2 = 0.318
the spectral errors:
Initially periodic comb structure
Optimized comb structure:
Towards superefficient quantum memory

## Slide 75
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv: 1706.00592
Towards superefficient quantum memory
1 4


1.42
1.42
Initial spectral comb structure:

## Slide 76
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv: 1706.00592,
1 4


1.42
1.42

|f()|2
1 4
Periodic final spectral comb structure:
Initial spectral comb structure:
Towards superefficient quantum memory

## Slide 77
S.A.Moiseev
2 0 1 4
KQC
_____________________________________________________________________________________
Kazan Quantum Center, KNRTU-KAI, Russia
N.S. Perminov and S.A. Moiseev Spectral-Topological Superefficient Quantum Memory. arXiv: 1706.00592,
1 4


1.42
1.42

|f()|2
1 4
Periodic final spectral comb structure:
Initial spectral comb structure:
Towards superefficient quantum memory

## Slide 78
N.S. Perminov, D.Yu. Tarankova, and S.A. Moiseev, Superefficient long-lived multiresonator quantum memory arxiv:1711.07014, (2017) .
Principal scheme of a hybrid MR QM
Towards long-lived superefficient quantum memory

## Slide 79
N.S. Perminov, D.Yu. Tarankova, and S.A. Moiseev, Superefficient long-lived multiresonator quantum memory arxiv:1711.07014, (2017) .
Principal scheme of a hybrid MR QM
Typical transmission spectra of HMR QM (recording stage) after spectral-topological optimization in wide frequency band
Towards long-lived superefficient quantum memory

## Slide 80
N.S. Perminov, D.Yu. Tarankova, and S.A. Moiseev, Superefficient long-lived multiresonator quantum memory arxiv:1711.07014, (2017) .
Principal scheme of a hybrid MR QM
Typical transmission spectra of HMR QM (recording stage) after spectral-topological optimization in wide frequency band
[1] We have shown that the broadband input signal is almost completely absorbed by several spin ensembles (with an inhomogeneous broadening less than the width of the signal field) with different central frequencies forming a comb.
[2] The efficiency of the transfer of the signal field to the spin system can reach 99.99% even under weak limitations for the parameters of energy losses within the multiresonator system.
[3] Proposed scheme is universal and can be used to combine several different types of QM devices into a single wideband QM block with a higher quality spectral profile.
Towards long-lived superefficient quantum memory

## Slide 81
N.S. Perminov, D. Yu. Tarankova, and S. A. Moiseev. Superefficient cascade multiresonator quantum memory Las. Phys. Lett (2018 in press) arXiv:1809.08759

## Slide 82
Выводы
______________________________________________________________________________
Казанский Квантовый Центр, КНИТУ-КАИ, Казань, Россия С.А. Моисеев
КП на фотонном эхо в резонаторе облегает возможность достижения высокой квантовой эффективности и реализации адресной памяти.
Экспериментально продемонстрирована реализация КП на фотонном эхе с естественным неоднородным уширением линии с эффективностью 13.6 %, также продемонстрировано сохранение до 10 световых импульсов, возможность запоминания фаз каждого импульса и возможность селективного восстановления отдельных импульсов, реализована КП на фотонном эхе в резонаторе с квантовой эффективностью 21 %. Полученные результаты позволяют сделать вывод о возможности реализации квантовой эффективности > 60 % в этой е схеме при использовании лучшего кристалла и более точной настройки оптического резонатора.
Выполнены первые эксперименты по фотонному эху в волноводе, сформированном внутри объема кристалла с редкоземельными ионами туллия. Эксперименты продемонстрировали технологические возможности для создания квантовой памяти на таких волноводных кристаллах.
Эксперименты по фотонному эху на кристаллах с редкоземельными ионами указывают на реальные перспективы создания высокоэффективной многомодовой КП, которая может быть использована для создания оптических квантовых репитеров.
О квантовой памяти на фотонном эхе

## Slide 83
Выводы
Системы резонаторов открывают путь в создании высоэффективного интерфейса для сохранения широкополосных световых полей.
Есть возможность создания МР КП в оптическом и микроволновом спектральном диапазоне (последняя продемонстрировала интересные перспективы для достижения высокой квантовой эффективности).
МР схема может обеспечить сверхэффективное сохранение квантового сигнала, что представляется возможным для экспериментальной реализации в условиях, характерных для работы сверхпроводящего квантового компьютера.
Показана возможность реализации долгоживущей МР КП при дополнительном использовании ансамбля спинов в системе минирезонаторов.
______________________________________________________________________________
Казанский Квантовый Центр, КНИТУ-КАИ, Казань, Россия С.А. Моисеев
О многорезонаторной (МР) квантовой памяти

## Slide 84
http:/kazanqc.org
№ 14-12-01333 П
Казанский Квантовый Центр, Казанский Национальный Исследовательский
Технический Университет им. А.Н. Туполева, Четаева 18а, Казань, Россия
Грант правительства РФ № 14.Z50.31.0040, 17.02.2017
Лаборатории ККЦ КНИТУ-КАИ:
Квантовой памяти (С.А. Моиссеев)
Фотоники и квантовых технологий (А.М. Желтиков)
Квантовых коммуникаций (А.В. Глейм)

## Slide 85
Kazan
Thank you for your attention !

## Slide 86
2 0 1 4
KQC
Схема установки по наблюдению фотонного эха, 2015 год. Квантовый центр КНИТУ-КАИ
Рис. 1. Схема установки для наблюдения фотонного эха для двух диапазонов длин волн. PD – фотодетектор; APD – лавинный фотодиод; GT – поляризатор Глана-Тейлора; BS – делитель пучка; AOM – акустооптический модулятор; стрелками показаны откидные зеркала. Управление акустооптическими модуляторами осуществляется при помощи генератора сигналов произвольной формы. Регистрация сигналов осуществляется цифровым осциллографом с частотной полосой пропускания 1 ГГц. Источниками излучения служат одночастотные лазеры. Стол над лазерами помещен в локальную систему очистки воздуха..
На пути к реализации оптической квантовой памяти на фотонном эхе в резонаторе
на нерезонансных рамановских переходах в твердом теле
Optical cryostat, Temperature > 1.3 K
Optical cryostat, Temperature >3.7 K
Stabilized lasers for visible spectral range